## Slide 1
<number>
Chapter- 2
OTFT Parameters, Structures, Models, Materials, Fabrication and Applications - A Review

## Slide 2
Introduction
Motivation Behind this Emerging Research Area
Organic Thin Film Transistor
OTFT Operating Principle, Its Advantages and Applications
OTFT Structures
OTFT Characteristic Parameters
Organic Semiconductor Materials Basics
Other Materials Required for OTFTs
Fabrication
Summary
<number>
Outline of the Chapter
Organic Thin Film Transistor: Materials to Circuits
Notes: <number>

## Slide 3: Important Landmarks and Introduction
Researchers realized in 1970 that some applications, like displays, RFID tags, required large array of low cost electronics which was not possible with silicon.
This marked the advent of amorphous silicon TFTs (a-Si-TFTs).
Discovery and Development of the conducting polymers (Polyacetylene-pure state is poor conductor+I2) by Dr. H. Shirakawa, Dr. Alan G. MacDiarmid and Dr. Alan. J. Heeger created a new research field in 1976.
Organic Semiconductor Materials:
Conducting Polymers: Polythiophene group (P3HT, P3OT, P3AT)
Small Molecules: Pentacene, CuPc, PCBM, F16CuPC.
First Organic / Polymer Thin Film Transistor (OTFT/PTFT) was demonstrated properly – 1986.
<number>
Organic Thin Film Transistor: Materials to Circuits
Notes: <number>

## Slide 4
<number>
OTFTs provide various important benefits over TFTs and MOSFET/CMOS based on inorganic semiconductor materials:
Mechanical flexibility: Foldable, Bendable, Lightweight
Compatibility with plastic substances
Organic displays are relatively cheap.
Polymer based TFTs with electrical characteristics comparable to or better than (a-Si-H) TFTs devices have been demonstrated.
Does not require a glass substrate as amorphous silicon does.
Chemical tunability of conducting polymers.
Easy integration in different device applications.
Ecological and economic benefits.
Motivation and Why OTFT??
Organic Thin Film Transistor: Materials to Circuits

## Slide 5: Classification of OTFTs Structures
Organic Thin Film Transistors (OTFT)
Bottom Gate (BG)
Dual Gate (DG)
Top Gate (TG)
Bottom Gate (BG)
<number>
Single Gate (SG)
Multi- Gate (MG)
Top Gate (TG)
Organic Thin Film Transistor: Materials to Circuits
Notes: <number>

## Slide 6: Classification of Single Gate OTFT Structures
SG-OTFT
Bottom Gate (BG)
Bottom Gate-Bottom Contact (BGBC)
Top Gate (TG)
Bottom Gate-Top Contact (BGTC)
<number>
Top Gate-Top Contact
(TGTC)
Top Gate-Bottom contact
(TGBC)
Organic Thin Film Transistor: Materials to Circuits
Notes: <number>

## Slide 7
Compatibility with plastic substances
Lower-cost deposition process
Lower temperature manufacturing (60-120oC)
<number>
Transistor having organic semiconductor (small molecules/ conducting polymers) as active layer to current flow.
Organic Thin Film Transistor
Organic Thin Film Transistor: Materials to Circuits

## Slide 8
16
BGTC |  | Low Contact Resistance. High Mobility. High Current Larger Channel Length
BGBC |  | High Contact Resistance Low Mobility. Low Current. Easy to Fabricate.
Comparison of BGTC and BGBCOTFTs Structures
Organic Thin Film Transistor: Materials to Circuits

## Slide 9
16
TGBC |  | Tough Fabrication. Low Contact Resistance
TGBC |  | Easy to Fabricate. High Contact Resistance. Similar to MOSFET.
Comparison of TGBC and TGTC OTFTs Structures
Organic Thin Film Transistor: Materials to Circuits

## Slide 10: Difference Between Organic and Inorganic Material
S.N. | ORGANIC MATERIAL | INORGANIC MATERIAL
1. OSC | Polymer/Small molecule based organic material | Silicon based inorganic material
2. Charge carriers: | Polarons and Excitons | Charge carriers through electrons, holes and ions.
3. Charge Transport: | Hopping | Energy band gap
4. Mobility: | 10-6 -5 cm2/V.s | 10-2 - 10-4 cm2/V.s
5. Bonding: | Ionic, Covalent and Van-der waal force | Ionic, Covalent, metallic
6. Cost: | $ 5/ft2 | $ 100/ft2
7. Fabrication Cost: | Low capital | $1 - $ 10 billion
8.Temperature Range: | Low temp (30 – 1200 C) | Greater than 10500 C
9. Device Size: | 10ft X Roll to Roll | Less than 1m2
10.Substrate | Flexible Plastic Substrate | Rigid Glass or Metal
Organic Thin Film Transistor: Materials to Circuits
Notes: <number>

## Slide 11
S. N. | ORGANIC MATERIAL | INORGANIC MATERIAL
11.Process Conditions: | Ambient processing | Ultra Clean Room
12. Process: | Continuous direct printing | Multi–step photo lithography
13. Biodegradability: | Biodegradable being made from carbon | Non biodegradable
14. Compatibility: | With flexible or plastic substrates | Non compatible with plastic or flexible substrate
15. Free Carriers: | Do not support free electrons and holes instead have Polarons and excitons | Free carriers in form of electrons and holes.
16. Effective Mass: | Huge | Less
Organic Thin Film Transistor: Materials to Circuits
Notes: <number>

## Slide 12: OTFTs Performance Parameters
Transfer (Id-Vg) Curve
Field Effect Mobility (μ) [cm2/V.s]
Sub-threshold Slope (SS)
Threshold Voltage (VTh)
On/Off Current Ratio (Ion/Ioff)
Performance Parameters
at saturation region
<number>
Transconductance (gm)
Performance of an OTFT is characterized in terms of several conventional parameters, including
Field effect mobility,
Threshold voltage,
On/off current ratio
Sub-threshold slope
Transconductance
Organic Thin Film Transistor: Materials to Circuits

## Slide 13
Factors Influencing OTFTs Performance
Performance Parameters | Dominant Factors
Mobility (High) | Fabrication Technique, Impurity, Gate Biasing, Material for Semiconductor
On – Current (High) | W/L , Mobility, Contact Resistance, Channel Length
Off - Current (Low) | W/L, Gate Insulator, Contact Resistance
Threshold Voltage (Low) | Channel Length, Thickness of Semiconductor Layer
Sub-Threshold Slope (Steep Slope) | Capacitance & Thickness of Insulator Drain /Source and Gate Biasing
Contact Resistance (Low) | Structure of PTFT Channel Width
<number>
Organic Thin Film Transistor: Materials to Circuits

## Slide 14
Target: > 1 cm2/Vs on/off ratio >106 for n type or p/n type Organic Semiconductors
Conjugated π-Electron System, High Electron Affinity ( for n type) or ambipolar Characteristics (for p/n type)
Good Intermolecular Electronic Overlap
Good Film Forming Properties
Chemical Purity
Stability
Material Requirements for OTFTs
<number>
Organic Thin Film Transistor: Materials to Circuits

## Slide 15
Materials | Organic ( PTFTs / OTFTS/OFETs) | Inorganic (MOSFETs/TFTs)
Substrate | PET-Polyethylene Terephthlate, PEN –Polyethylene Naphthalate, Klauk et al. 2003etc.(High Toughness & thermal resistance, Flexibility, Light weight) | Silicon wafer (High Melting Point, good flatness, Low Diffusivity of chemical)
Contact Electrodes | Gold,Platinum,Al,Mg,Pd source/drain metal with large work function matched with either HOMO or LUMO. Polymer contact-PEDOT:PSS | Metals (Au, Cu)
Semiconducting Layer (Channel/ Thin Film) | Organic Semiconducting material with electrical characteristics P3HT- Poly(-3-hexylthiophene), P3AT-Poly (3-alkylthiophene) P3OT- poly (3-octylthiophene) Pentacene: good electrical Propt.) | a-Si:H, Si
Dielectric layer | Gate insulating layer with high dielectric constant and high resistivity (PMMA-Polymethyle methacrylate ) | Insulating Materials SiO2, TiO2, Al2O3
<number>
Organic and Inorganic Device Materials
Organic Thin Film Transistor: Materials to Circuits
Notes: <number>

## Slide 16
Organic Semiconductors
Organic semiconductors are classified as the conducting polymers and small molecules.
Mobility of polymers is found lower than small molecules due to higher molecular weight.
To obtain it higher; the grains of semiconductor should be larger in size.
Performance of Polymer transistor (PTFTs/OTFTs) critically depends on the chemical and structural ordering of the chains at interface of OSC-insulator.
Important Influencing Factors
Interface of metal and dielectric with semiconductor
Ordered molecular structure of the active layer
Efficient injection at contacts and stability.
Organic Thin Film Transistor: Materials to Circuits

## Slide 17: Organic Semiconductor Material Basics
An organic semiconductor is an organic material with semiconductor properties.
Molecular conjugation :The fundamental property that allows organic molecules to conduct electronic charge.
Conjugation causes Delocalization and allow charge transport.
Organic Semiconductor materials categories as:
Polycyclic aromatic compounds(e.g. Pentacene, anthracene, etc)
Polymeric organic semiconductors(e.g. Poly(3-hexylthiophene, etc )
8
Organic Thin Film Transistor: Materials to Circuits

## Slide 18: Electronic structure of Organic semiconductor
<number>
Fig. (a) sp2 hybridization of two carbon atoms and (b) Bonding of pz orbitals.
Organic Thin Film Transistor: Materials to Circuits

## Slide 19
Organic Semiconductor
Inorganic Semiconductor
Weak Van der Waals interaction forces
π-bond overlapping
Molecular gas property (molecule’s identity)
Hopping type charge transport dominant
Low mobility and small mean free path
Strong covalent bonds
σ-bond
Only crystal property
Band type charge transport dominant
High mobility and large mean free path
<number>
Organic and Inorganic Semiconductors
Organic Thin Film Transistor: Materials to Circuits

## Slide 20
Small Molecules
Most extensively used p-type Small molecule OSCs are
Pentacene
6,13-bis_triisopropyl-silylethynyl (TIPS) pentacene
Tetracene
Pentacene and its derivatives are the most promising and extensively used materials due to highest mobility.
Its deposition on dielectric SiO2 yielded higher carrier mobility.
P-type Organic Semiconductors
Chemical Structure of Pentacene small molecule Semiconductor
Organic Thin Film Transistor: Materials to Circuits

## Slide 21
P-type Organic Semiconductors
Conducting Polymers
Most extensively used p-type conducting polymers are
PA - Polyacetylene
Polythiophene
Polyfluorene
P3AT - Poly (3-alkylthiophene)
P3HT - Poly(-3-hexylthiophene)
P3OT - poly (3-octylthiophene)
PQT-12 - Poly 3, 3΄΄-dialkylquarterthiophene
F8T2 - Poly-9, 9’ dioctyl-fluorene-co-bithiophene
Organic Thin Film Transistor: Materials to Circuits

## Slide 22
N-type Organic Semiconductors
p and n-type OSCs are required to design the complementary inverters that are beneficial for low power consumption, higher noise margin and better stability.
Therefore, the development of n-type semiconductors is equally important.
There is an optimum thermodynamic stability window in n-type doped materials.
It strongly depends on the free energy of activation that is associated with the chemical process/reaction with either water or oxygen.
While designing these devices, the semiconductor must be utilized which, can allow the injection of electrons into its LUMO.
Organic Thin Film Transistor: Materials to Circuits

## Slide 23
Ambipolar Materials OSCs
In the literature, the majority of OTFTs is demonstrated either by p or n-type semiconductors.
To achieve the organic complementary technology either n and p-type transistors can be incorporated by electrical connection or ambipolar charge transport can be realized in a single transistor.
Researchers reported high gain inverter with a natural pigment- Indigo, which contains the balanced electron and hole mobility and good stability against the degradation in air.
Organic Thin Film Transistor: Materials to Circuits

## Slide 24
Source and Drain Electrode Materials
Electrodes can be fabricated using either inorganic or organic materials.
Contact metal for source (S) and drain (D) should contain low interface barrier with active layer to inject a large number of carriers.
Contacts must possess a small resistance.
Contact Electrode can be fabricated by thermal evaporation method.
Adding Ni on Au improves the adhesion of gold on oxide, whereas, Pt electrodes are inferior comparatively.
Organic Thin Film Transistor: Materials to Circuits

## Slide 25
Electrode Materials | Work function (eV)
Au (Gold) | 5.1
Cu (Copper) | 4.7
Ag (Silver) | 4.0
Cr (Chromium) | 4.5
Al (Aluminum) | 4.0 - 4.28
Ni (Nickel) | 5.0 - 5.22
Ti (Titanium) | 3.84
Pt (Platinum) | 5.65
Ca (Calcium) | 2.87
Co (Cobalt) | 5.0
Fe (Iron) | 5.0
Work Function of S/D Contact Electrodes
Organic Thin Film Transistor: Materials to Circuits

## Slide 26
Gate Electrode Materials
Selection of material for gate (G) electrode should be based on good adhesion and patterning capabilities to the substrate and gate dielectric.
Gate metal work function should be comparable to the active semiconductor layer to attain lower threshold voltage (Vt).
Such materials include heavily doped silicon, Al, Au, indium tin oxide (ITO) etc.
Organic Thin Film Transistor: Materials to Circuits

## Slide 27
Gate Dielectric Materials
Insulator material needs to have very high resistance to prevent the leakage between gate and channel.
High dielectric constant to achieve enough capacitance (Ci) for channel current flow.
High dielectric constant insulators result in lower switching voltage and elevated current capabilities.
Organic polymers
PMMA
PVP
PI
PVA
Demonstrate good process ability and dielectric properties
Organic Thin Film Transistor: Materials to Circuits

## Slide 28
Inorganic Gate Dielectric Materials
Currently, the researchers are focusing to enhance the properties of dielectric materials, since it is extremely crucial to achieve the reliability and high-performance.
Dielectric materials should have the compatibility with OSCs, these materials should exhibit high insulation also.
High resistivity reduces the interface trap density between OSC and gate dielectric which, in turn prevents the leakage
Organic Thin Film Transistor: Materials to Circuits

## Slide 29
Substrate Materials
Most of the OTFTs are fabricated on a heavily doped silicon substrate to achieve the film of SiO2 dielectric with ease of oxidation.
Si is often used in electronics not only for its intrinsic properties but also for its good interface with thermally grown oxide.
Organic substrates like poly ethylene-naphthalate have shown remarkable performance in term of flexibility that motivates the researchers for its utilization in flexible electronic devices and circuits.
Organic Thin Film Transistor: Materials to Circuits

## Slide 30: Limitations of Organic Material
Organic semiconductors are very soft and sophisticated.
Organic Materials degrade and can break easily .
Characteristics of organic materials changes with environmental conditions after long duration.
Most of instability comes from chemical structure of compounds.
Lower mobility and switching speed compared to silicon based devices
Due to low mobility, it is limited to low speed applications.
<number>
Organic Thin Film Transistor: Materials to Circuits
Notes: <number>

## Slide 31
<number>
Performance of p and n-type OSC Materials in terms of Mobility
Comparative plot of mobility
growth for p- and n-type OSCs
Comparative plot for growth in mobility of p- and n-type transistors w. r. t. fabrication processes.
Organic Thin Film Transistor: Materials to Circuits

## Slide 32: Basic Fabrication Steps SG-OTFT (BGBC)
<number>
Organic Thin Film Transistor: Materials to Circuits

## Slide 33: Basic Fabrication Steps SG-OTFT (BGTC)
Organic Semiconductor
Material: Small molecules/conducting polymers
Process: Thermal evaporation/ solution processing
Gate Metal
Materials: Organic/inorganic
Process: Vacuum thermal evaporation/solution processing.
Gate Dielectric
Materials: Organic/inorganic
Process: Thermal evaporation/solution processing
Source/Drain Contact
Materials: Organic/inorganic
Process: Shadow masking/lithography/lift-off/transfer printing
Passivation Layer
Materials: Organic/inorganic insulator
Process: CVD, Dry Etching, RIE: Reactive ion etching
Substrate
Materials: Heavily doped Si wafer /glass /plastic or organic compatible material
Process: RCA cleaning/cleaning by suitable solution
Organic Thin Film Transistor: Materials to Circuits
Notes: <number>

## Slide 34
Flexible
OLED
Flexible
LCD
Organic
Memory
Image
Sensor
Bio-
Sensor
Organic
Laser
Smart Card
RFID Tag
E-paper
OTFT
IC
Technology
Optical
Technology
Bio
Technology
Apparel
Technology
Sensor
Technology
Memory device
Technology
LCD
Technology
OLED
Technology
E-Paper
Technology
Electrical
Fabric
<number>
Organic TFT Applications

## Slide 35
<number>
Scaling is not very much effective in OTFT due to their lower drive current
Effect of scaling is almost similar in both OTFT and MOSFET devices
Current in OTFT reduces by the scaling factor in full scaling that in turn degrades the switching behavior
Constant voltage scaling increases the drain current and power density too
OTFTs are strongly affected by the contact resistance that becomes increasingly evident as the channel length is scaled down
Effect of Scaling on OTFT Parameters and Performance
Organic Thin Film Transistor: Materials to Circuits
Notes: <number>

## Slide 36
<number>
Characteristics of OSCs alters with time and ecological environment due to their susceptibility to water and oxygen under ambient conditions
Several n-channel TFTs processed and tested under inert condition only
Numerous issues are still open ended, specifically those associated with the stability and performance variation from roll to roll and device to device
Optimization of fabrication methodology and synthesis of novel materials, the lifetime/durability can be undoubtedly increased
Through encapsulation of the devices, longer functioning lifetime can be achieved
Due care must be taken against exposure of devices to moisture and oxygen, which can be achieved by depositing a film of inorganic oxides and special protective coatings.
Lifetime and Durability of Organic Semiconductors
Organic Thin Film Transistor: Materials to Circuits

## Slide 37
<number>
Improvement in Stability, lifetime and durability
Cost economy, temperature dependency, operating bias and power dissipation
Miniaturization
Look for high performance OSCs, electrode, dielectric and substrate materials and novel OTFT structures
Surface treatment and self-assembled monolayer of the dielectric
High doping region near the contacts and additional OSC layer between contact and OSC.
Steps Needed for OTFTs to be Commercialized on a Larger Scale
Organic Thin Film Transistor: Materials to Circuits

## Slide 38: Summary
Organic transistor boasts of a bright future with a wide spectrum of applications.
It is required to develop suitable models to adequately understand the OTFTs behavior..
To investigate the impact of active and dielectric layers thickness on the performance of both top and bottom contact structures individually
It is strongly required to develop techniques that can substantially improve the performance of organic digital circuits.
Organic Thin Film Transistor: Materials to Circuits
Notes: <number>