## Slide 1: 4th Ed Cpt 2 Polymer Structure

## Slide 2: Table 2.1 Typical properties of straight chain hydrocarbons.
Average number Boiling Name Physical state Typical
of carbon atoms range,oC at room temp. uses
1-4 <30 Gas Gas Heating
5-10 30-180 Gasoline Liquid Automotive fuel
11-12 180-230 Kerosene Liquid Jet fuel, heating
13-17 230-300 Light gas oil Liquid Diesel fuel, heating
18-25 305-400 Heavy gas oil Viscous liquid Heating
26-50 Decomposes Wax Waxy Wax candles
50-1000 Decomposes Tough waxy to solid Wax coatings food containers
1000-5000 Decomposes Polyethylene Solid Bottles, containers, films
>5000 Decomposes Polyethylene Solid Waste bags, ballistic wear, fibers, automotive parts,
truck liners

## Slide 3: Figure 2.1 Simulated structure of high-density polyethylene (HDPE), left, contrasted with the structural formula of linear or normal decane, right.

## Slide 4: Figure 2.2 Simulated structural formula for branched low-density polyethylene (LDPE); compare with Figure 2.1 for HDPE.

## Slide 5: Table 2.2 Types of Commercial Polyethylene
General structure %-Crystallinity Density (g/cc)
LDPE-Linear with branching 50 0.92-0.94
LLDPE-Linear with less branching 50 0.92-0.94
HDPE -Linear with little branching 90 0.95

## Slide 6: Figure 2.3 Skeletal structural formulas of a linear polymer (left), and a network (crosslinked) polymer with low crosslinking density (middle) and high density crosslinking (right). Cross-link sites are noted by the non-darkened spheres.

## Slide 7: Figure 2.4 Simulated structural formulas showing the usual head-to-tail, middle, and unusual head-to-head, right, configurations of polypropylene.

## Slide 8: Figure 2.5 Skeletal formulas of isotactic (top), syndiotactic (middle), and atactic (bottom) of poly(vinyl chloride), PVC.

## Slide 9: Erythrodiisotactic Threodiisotactic Erythrodisyndiotactic Threodisyndiotactic
Figure 2.6 Simulated formulas of ditactic isomers where R2 are chain extensions and R and R1 are not hydrogen.

## Slide 10
Figure 2.7 Newman projections of designated conformers of n-butane- Anti (left), Eclipsed (middle) and Gauche (right).

## Slide 11: Figure 2.8 Representation of a crystalline portion from isotactic polypropylene, left, and an amorphous portion from atactic polypropylene, right.

## Slide 12: Table 2.2b. General classes of secondary forces.
Type Relative Strength
Ion-dipole Strongest
Dipole-dipole
Dipole-induced dipole
Induces dipole-induced dipole Weakest

## Slide 13: Figure 2.9 Typical hydrogen-bonding (shown as “-“ between hydrogen on nitrogen and oxygen for nylon 66.

## Slide 14: Table 2.3 Critical chain lengths for some common polymers.
Polymer Critical Chain Length
(Number of repeat units)
Polycarbonate 20
1,4-Polybutadiene 110
Poly(decamethylene adipate) 11
Polydimethylsiloxane 450
Polyethylene 150
Poly(ethylene oxide) 100
Poly(methyl methacrylate) 160
Polypropylene 170
Poly(propylene oxide) 100
Polystyrene 300
Poly(vinyl acetate) 250
Poly(vinyl alcohol) 170
Poly(vinyl chloride) 175
modified from L. H. Sperling, Introduction to Physical Polymer Science, 4th Edition, Wiley, Hoboken, NJ,

## Slide 15: Figure 2.10 Determination of Tg by noting the abrupt change in specific volume.

## Slide 16: Table 2.4 Approximate Glass Transition Temperatures (Tg) for Selected Polymers
Polymer Tg (K) Polymer Tg (K)
Cellulose acetate butyrate 323 Cellulose triacetate 430
Polyethylene (LDPE) 148 Polytetrafluoroethylene 160,400a
a-Polypropylene 253 Poly(ethyl acrylate) 249
i-Polypropylene 373 Poly(methyl acrylate) 279
Polyacrylonitrile 378 alpha-Poly(butyl methacrylate) 339
Poly(vinyl acetate) 301 alpha-Poly(methyl acrylate) 378
Poly(vinyl alcohol) 358 Poly(vinyl chloride) 354
cis-Poly-1,3-butadiene 165 Nylon-66 330
trans-Poly-1,3-butadiene 255 Poly(ethylene adipate) 223
Polydimethylsiloxane 150 Poly(ethylene terephthalate) 342
Polystyrene 373
a. Two major transitions observed.

## Slide 17: Figure 2.11 Typical DSC thermogram of a polymer.

## Slide 18: Figure 2.12 End-to-end distances for four 30-unit chains.

## Slide 19: Figure 2.13 Helical conformation of isotactic vinyl polymers. (From N. Gaylord, in Linear and Steroregular Addition Polymers (N. Gaylord and H. Mark, eds.), Wiley, NY, 1959.

## Slide 20: Figure 2.14 Schematic two-dimensional representation of a modified micelle model of the crystalline-amorphous structure of polymers.

## Slide 21: Figure 2.15 Structure of a spherulite from the bulk. Bottom shows a slice of a simple spherulite. As further growth occurs, filling in, branch points, etc. occur as shown above (top). The contour lines are simply the hairpin turning points for the folded chains.

## Slide 22: Figure 2.16 Spherulite structure showing the molecular-level lamellar chain-folded platelets and tie and frayed chain arrangements, left, and a more complete model of two sets of three lamellar chain-folded platelets formed from polyethylene, right. Each platelet contains about 850 ethylene units as shown here.

## Slide 23: Figure 2.17 Crystalline polymer structures formed under applied tension including flow conditions. Middle shows the tertiary mono-fibrilar structure including platelets and at the left shows these mono-fibrilar structures bundled together forming a quaternary structure fibril. Right shows the distorted shish kebab formed with more rapid flow.

## Slide 24: Figure 2.18 Elongation of an elastomer as a function of applied force, stress, where A is the original “relaxed” state, B represents movement to full extension, C is the point at which the elastomer “breaks”, and D represents force necessary to pull two separate pieces of elastomer apart.

## Slide 25: Figure 2.19 Idealized structure illustrating crystalline (ordered) and amorphous (nonordered) regions of lightly branched polyethylene chains for a prestressed and stressed orientation.

## Slide 26: Figure 2.20 General physical states of materials as a function of crystallinity and molecular weight.

## Slide 27: Table 2.6. General property correlations with Tg.
Cross-linked elastomers Above Tg
Linear (or branched) amorphous adhesives Above Tg
Amorphous plastics Generally above Tg
Largely crystalline plastics Generally above Tg,Below Tm
Crystalline fibers Below Tm
Coatings At or near Tg

## Slide 28: Figure 2.21 Chemical cross-linking of cis-1,4-butadiene through reaction with sulfur.

## Slide 29: Figure 2.22 Illustration of two types of physical cross-linking-chain entanglement and crystalline regions.